## Slide 1
SYSTEM ON PACKAGE USER GROUP
General Chairs: Anita Madan – Independent Consultant
Daminda Dahanayaka - GLOBALFOUNDRIES
Special Thanks to Ted Kolasa !

## Slide 2
AGENDA

## Slide 3: Agenda
2 hrs and 15 minute session
  Introduction – Ted Kolasa
    Introduction to User Group Series
    2021 virtual conference metrics
    Survey questions on the ISTFA app
    ASM Connect introduction
    Introduce User Group Chairs
  User Group Discussion
    Speakers (discussion starters)
    General discussion
    FA Roadmap preview

## Slide 4: USER GROUP SESSIONS
An opportunity to share information and discover avenues for future collaboration.
Open forum with initiated topics, and a robust interchange of ideas.
Share what you know, enquire about something new, challenge the status quo.
While the moderators provide an initial framework to get the discussion going, this is very much YOUR event.
Continue your discussions at the ASM CONNECT Community page
https://connect.asminternational.org/electronicdevicefailureanalysissociety/communities/

## Slide 5: ISTFA USER GROUP SESSIONS
Tuesday November 2nd: 2:45 PM – 5:00 PM
Sample Prep User Group – 101 A to C
- Chair, Jim Colvin, FA Instruments, Inc
- Co-chair, Cecile Bonifacio, Fischione Instruments
- Co-chair, Kah Chin Cheong, Samsung Austin Semiconductor LLC.
- Co-chair, Nathan Bakken, Intel
System on Package User Group – 102 A to C
- Chair, Lihong Cao, ASE
- Co-chair, Kevin Distelhurst, GlobalFoundries
- Co-chair, Wentao Qin, onsemi

## Slide 6: ISTFA USER GROUP SESSIONS
Wednesday November 3rd: 2:45 PM – 5:00 PM
Contactless probing and Nanoprobing User Group – 101 A to C
- Chair, Dan Bockelman, Intel
- Co-chair, Neel Leslie, Thermo Fisher
- Co-chair, Sara Ostrowski, EAG
FIB User Group – 102 A to C
- Chair, Steven Herschbein, Independent Consultant
- Co-chair, Valerie Brogden, University of Oregon
- Co-chair, Michael Wong, Thermo Fisher
- Co-chair, Edward Principe, Synchrotron Research

## Slide 7
HIGHLIGHTS FROM Jan 25-28, 2021 VIRTUAL MEETING
Chairs and co-chairs
  System-on-Package - Kevin Distelhurst (GF) and Prasad Divekar (Intel)
  Sample Preparation - Jim Colvin ( FA Instruments) and Bryan Tracy ( Tesla)
  Nanoprobing/Optical Probing and SPM - Daminda Dahanayaka(GF), Dan Bockelman (Intel), Neel Leslie (Thermo Fisher) and Sara Ostrowski, (EAG)
  FIB/Chip Edit - Steven Herschbein (Individual contributor), Michael Wong (Thermo Fisher) and Valerie Brogden (University of Oregon)
Participation:
  Semiconductor companies - Globalfoundries, Intel, AMD, NXP, Maxim Integrated, IBM, Infineon, Micron, Marvell, onsemi, Maxim Integrated
  Vendor companies – Thermo Fisher, Carl Zeiss, Hitachi, Allied High Tech, and many more
  University Attendees - University of Florida, McMaster University, Iowa State University, University or Oregon, Tech University Berlin Germany
  International participation - US, Germany, Singapore, Israel
Totally Virtual !
Recordings available on the ASM Connect page
Chart: Number Attended
| Number attended
System on Package (77) | 77
Sample Preparation (165) | 165
Contactless Probing and Nanoprobing (145) | 145
FIB (134) | 134

## Slide 8: ASM CONNECT SITE
Communities have been created on ASM Connect for each User Group.
Continued discussion after User Group Series – if you are not a member, you will get an invite to join the communities
https://connect.asminternational.org/search?executeSearch=true&SearchTerm=edfas&cs=Communities

## Slide 9
System on Package User Group Chairs Introduction
Chair: Lihong Cao, ASE
Co-Chair: Kevin Distelhurst, GlobalFoundries
Co-Chair: Wentao Qin, onsemi

## Slide 10: Chair – Lihong Cao – ASE (US) INC.
Dr. Lihong Cao is a Director in ASE Group responsible for advanced packaging technology development (2.5D/3D, FOCoS, PoP, SIP), new product introduction, strategic planning, and business engagement.
Her expertise and experience span from design, process development, qualification, and production enablement especially in HPC and AI/ML.
Prior to joining ASE, as a Sr. Manager in AMD, she led global package analysis operations and failure analysis to support product development, qualification, production and customer issues. She was also in charge of advanced package failure analysis technique development and roadmap
Lihong also had academic and professional experience in Nanyang Technology Univ. in Singapore. She has published more than 80 technical papers. She has been a Technical Chair and Tutor in ISTFA since 2011. She was invited as panel members in ISTFA 2018 & 2019.

## Slide 11: Co-chair – Kevin Distelhurst – GlobalFoundries
MTS Failure Analysis Engineer at GLOBALFOUNDRIES for 8+ years
  FAB9 – Essex Junction, Vermont
  Formerly IBM microelectronics division
Team lead that oversees the entire FA process of a submission
    Focus from ASIC to analog/RF, all fail types
    Qualifications – RMA – Yield
  Focus on several techniques; publications related to those
  2.5D packaging fault isolation and analysis
  Magnetic Field Imaging
  EBIC/EBAC
  Diving deeper into PEM and laser-based techniques now
Drives scholarly (publications, patents, newsletters) and development activities with colleagues
  Attends ISTFA every year for the past several years
  EDFAS volunteer

## Slide 12: Co-Chair – Wentao Qin – onsemi
Ph. D. in Physics, University of Missouri-Rolla
Phase transformation, solid-state reaction, corrosion, electron microscopy (TEM & SEM)
TEM & materials science engineer in Motorola/Freescale & currently onsemi
Patents on packaging
Journal publications in Microscopy and Microanalysis, Microelectronic Reliability, Ultramicroscopy, Nature Communication, Nano Energy, Nano Letters, etc.
Editor, with Dr. Yan Li, special issue of “The Reliability of Advanced Microelectronic Packaging”, IEEE TRANSACTIONS ON CPMT, 2020
1st place awards, EDFAS Photo Contests
Outstanding paper, ISTFA 2015

## Slide 13
EDFAS FA Technology Roadmap
ISTFA 2021 - User Group Summary
Dr. Keith Serrels
NXP Semiconductors, Austin, TX
keith.serrels@nxp.com

## Slide 14: FA Roadmap Background
Roadmap Mandate:
Identify both current and future FA challenges as part of an industry-wide gap analysis
Pursue potential solutions from both equipment providers and academic labs
Challenge:
Initial Roadmap structure (2019-2020) captured some key features, however…
  Offered limited technical detail and scope
  Commanded limited investment from FA community
 Needed to grow roots within the community to secure interest, generate momentum, and extract maximum value
Solution:
Created focused groups to authenticate technical gaps, communicate narrative, and drive content creation
Roadmap ownership across the community!!
 New council structure has been approved by the EDFAS Board and ASM

## Slide 15: New FA Roadmap Council Structure
Alignment Mentor:
Felix Beaudoin (GlobalFoundries)
Chairs:
Christian Schmidt (NVIDIA)
Yan Li (Intel)
Themes:
Packaging and Assembly
3D Device FA
Board and System Level FA
Alignment Mentor:
Keith Serrels (NXP)
Chairs:
Lesly Endrinal (Qualcomm)
Szu Huat Goh (GlobalFoundries)
Themes:
Fault Isolation
Product Yield
Test
Diagnosis
Die-Level Roadmap Council
(DLRC)
Package Innovation Roadmap Council
(PIRC)
Alignment Mentor:
David Su (Formerly TSMC)
Chairs:
Vinod Narang (AMD)
Chuan Zhang (NVIDIA)
Themes:
Nanoprobing
Microscopy
Scanning Probe Analysis
FIB Circuit Analysis & Edit
Isolation Domain
Post-Isolation Domain
Sample Preparation and Device Processing FIB Sample Preparation
Alignment Mentor:
Ryan Ross (JPL)
Chairs:
Nicholas Antoniou (Prime Nano)
Brendan Foran (Aerospace Corp.)
Themes:
Future Technologies
(Logic, Memory, Packaging)
FA Future Roadmap Council (FAFRC)

## Slide 16: Council Responsibilities / Community Requests
Each Council will collaborate with their internal committee members to:
  Accurately detail and rank the relevant technical challenges for their respective themes
  Promote active vendor/academic participation to explore and categorize potential solutions
  Communicate findings to FA community on Council-specific ASM CONNECT platforms
    Expanded gap analyses
    Technical whitepapers
  Councils have been activated and will issue their first round of findings during Fall 2022
Need involvement from wider FA community also
  Everyone is encouraged to participate
  Discuss relevant technical challenges/solutions at the ISTFA User Groups
  Initiate discussions on the ASM CONNECT community portals for each Council
    Watch the ISTFA 2021 FA Roadmap Update video
    Access links to the 4 Council-specific community platforms on the EDFAS Homepage on ASM CONNECT
    https://connect.asminternational.org/edfas/home
  Engage directly by emailing comments/questions directly to the Council Chairs (use above link)
  This is an international effort
    Both IPFA (Asia-Pacific) and the CAM Workshop (Europe) will offer Roadmap discussions as part of their future program offerings

## Slide 17: SOP User Group
System-on-package (SoP) addresses the demand for complexity and performance by integrating multiple functional components from different technologies in one package.
Advanced package types (2.5D, 3D, HD Fanout, WLP, ect.) used in SoP attempt to address the performance demand by shortening critical signal paths, mix-match functionalities and uniquely enabling integration of different niche technologies.
SoP increases reliability risks and failure analysis complexity

## Slide 18: Interesting Discussions from Last Session
Sample size limits of tools
  60x60mm, 70x70mm, 80x80mm?
Damaging the sample during deprocessing Potential Solutions Discussed:
  Heating sample during processing
  Surrounding sample with support material (epoxy)
Dynamic Lock-In Thermography (LIT)
  Some success, more case studies needed
Chip repackaging possible after extraction from advanced package?

## Slide 19
Failure Analysis Challenges on SiP
Susan Li
Cypress Semiconductor Corp, An Infineon Technologies Company
ISTFA 2021, Oct. 31 to Nov. 4, Phoenix, Arizona

## Slide 20: Susan Li
Susan is a Director of Failure Analysis Engineering at Cypress Semiconductor Corp., an Infineon Technologies Company. She has more than 25 years experience and has expertise in failure analysis lab operations, failure analysis process and tools/technique development on Microprocessor, Memory, Wired/Wireless, and IoT products
Susan earned a Master’s Degree in Materials Science and Engineering from Carnegie Mellon University, Pittsburgh, Pennsylvania, and a B.S.E.E. Degree in Electrical Engineering from Peking University, China. She has published more than 30 papers at international conferences and is currently holding 20 US patents.
Susan has been working with ISTFA Organizing Committees in the past 15 years and IPFA Technical Program Steering Committees in the past 10 years. She served two terms as a board member for EDFAS.

## Slide 21
SiP vs. SoC
Functional Diversification
Reduced development cost
Shorted time-to-market

## Slide 22
Increasing Interconnect Density:
> 5x from QFN to WLP
multiple times increase for 3D stacked packages

## Slide 23
Front-end & Back-end Merge
Thru-Si-Via
eWLB and WLP
(embedded Wafer Level BGA
and Wafer Level Package)

## Slide 24
Challenges:
Process/Equipment
Materials/Substrates
Physicals of Packages
Methods/Cross-cut Needs
Failure analysis
  Testability
  Accessibility
  Tools/Techniques
  Fault Isolation
  Inspection
  Non-destructive
  Destructive

## Slide 25: System on Package (SiP) – Miniaturization of the Entire System
Cited from electronicdesign.com
Cited from aseglobal.com
System-in-Package with Various CSP Components Inside

## Slide 26: Challenges of Fault Isolation on SiP (System in Package)
Fault isolation required at multiple levels:
  PCB board to modules
  Modules to SiP devices
  SiP devices to IC components
Non-destructive/Destructive analysis:
  2D/3D or uCT X-ray
  SAM C-scan and Thru-scan
  TDR/EOTPR
  SDR/SQUID
  Thermal Lock-In Emission (ELITE)
  Mechanical Polishing/Micro-Probing
  Laser Ablation and FIB Cross-section
  TEM Elemental Mapping
The following case study will be used to demonstrate the challenges of fault isolation on a SiP device with a single open pin failure in the FCBGA package with an interposer that is mounted on a module attached to the system board

## Slide 27: Challenges of Fault Isolation on SiP (System in Package)
TDR analysis at board level, module level and FBGA
showed the open is near interposer to WLCSP bump
Layer-by-layer mechanical polishing and micro-probing confirmed the open is at the interface between Cu layer 2 to Via 1 in the interposer board
Suspected Failure Site

## Slide 28: Challenges of Fault Isolation on SiP (System in Package)
Mechanical cross-section followed by the plasma cleaning showed a very fine crack line at the suspected interface between Cu layer 2 to Via 1 in the interposer
FIB/TEM analysis confirmed the separated interface between Cu layer 2 to Via 1. EDX analysis indicated extra C content at the interface area.
Optical
SEM

## Slide 29: Challenges of Fault Isolation on SiP (System in Package)

## Slide 30
Heterogenous Packaging
Yan Li
Intel Corporation
ISTFA 2021, Oct. 31 to Nov. 4, Phoenix, Arizona

## Slide 31
Dr. Yan Li is currently a senior staff packaging engineer in Assembly Test and Technology Development Failure Analysis Lab of Intel Corporation located in Chandler, Arizona.
She received her Ph.D. degree in Materials Science and Engineering from Northwestern University in 2006.
She is a senior member and contributor of many international professional associations, such as Minerals Metals and Materials Society (TMS), American Society for Metals (ASM), and Electronic Device Failure Analysis Society (EDFAS).
She has published over 20 papers and two patents in the microelectronic packaging area. She is the co-editor of a semiconductor industry highly recognized book: “3D Microelectronic Packaging: From Fundamentals to Applications” by Springer.
Yan Li (Intel)

## Slide 32: Outline
Introduction
Heterogenous Packages and key components
Failure analysis challenges

## Slide 33: Why Heterogenous Packaging?
Moore’s law predicts the exponential growth of ICs since 1970s,
The exponential growth of lithography equipment cost since 1970s
Advanced Packaging techniques are utilized to meet the market needs
3D Microelectronic Packaging: From Architectures to Applications, 2nd edition, Springer, 2021, ISSN 1437-0387

## Slide 34: Heterogenous Packages
Integrated Fan-Out (InFO) -Package On Package (PoP) from TSMC
Embedded Multi-Die Interconnect Bridge (EMIB) from Intel
Foveros technology from Intel
AMD Radeon™ Fury
Chip-On-Wafer-On-Substrate (CoWoS) from TSMC
Apple A7 package; Package on Package
Smaller interconnects; Higher performance; Lower power consumption
3D Microelectronic Packaging: From Architectures to Applications, 2nd edition, Springer, 2021, ISSN 1437-0387

## Slide 35: Through Silicon Vias (TSV)
Key components for Heterogenous Packaging
3D Microelectronic Packaging: From Architectures to Applications, 2nd edition, Springer, 2021, ISSN 1437-0387

## Slide 36: Micro bumps
Key components for Heterogenous Packaging
3D Microelectronic Packaging: From Architectures to Applications, 2nd edition, Springer, 2021, ISSN 1437-0387
Schematic illustration of a typical Thermal Compression Bonding process

## Slide 37: Cu interconnects
Key components for Heterogenous Packaging
3D Microelectronic Packaging: From Architectures to Applications, 2nd edition, Springer, 2021, ISSN 1437-0387
Schematic of Hybrid bonding or Direct Bond Interconnect (DBI) technology from Xperi
SEM cross-sectional image of bump-less Cu-Cu bonded structure with 6μm pitch

## Slide 38: Failure analysis challenges
Multiple failures in one unit.
EFA: Each failure needs x, y, and z identification
PFA: artifact free and revealing fine features in a large area
Imaging: high resolution with large field of view
Material analysis: pinpoint organic materials with sub micron resolution
Technical point of view
3D Microelectronic Packaging: From Architectures to Applications, 2nd edition, Springer, 2021, ISSN 1437-0387
TEM

## Slide 39: Failure analysis challenges
Low cost
High through put time
High success rate
AI and automation
Business point of view
3D Microelectronic Packaging: From Architectures to Applications, 2nd edition, Springer, 2021, ISSN 1437-0387

## Slide 40
Original Article in EDFA Magazine November 2021 | Volume 23 | Issue 4
Authors: Douglas Hunt1, Daniel Bader1, Pascal Limbecker2, and Heiko Barth2
Presented here with permission: Kevin Distelhurst1
GLOBALFOUNDRIES 1Essex Junction, VT, US 2Dresden, Germany
System on Package User Group
Methods to Enable Fault Isolation on 2.5D Molded Interposer Packages

## Slide 41
Overmold once again obstructing analysis
Previous Discussion:
Underfill present around the bumps.
Bumps exposed using MIP.
Enabled EBAC & visual inspection.
MIP = CF4-Free Microwave Induced Plasma

## Slide 42
How to expose a perimeter via chain covered by overmold?
OPTION 1
OPTION 2

## Slide 43
EBAC Fault Isolation Enabled and Successful!
EBAC = Electron Beam Absorbed Current
Discussion points:
How would you remove the overmold?
Other fault isolation techniques enabled?
Potential fails that would require this process?

## Slide 44
System on Package User Group
Additional Topics

## Slide 45: Topics – Fault Isolation (cont.) Lock-In Thermography
Discuss successes using Lock-In Thermography to isolate defects
  Buried in 3D Stacks
  In the Interposer of a 2.5D module
  Encapsulated chips with blocking structures
Source: “Methods to Enable Fault Isolation on 2.5D Molded Interposer Packages”, EDFA Magazine November 2021 | Volume 23 | Issue 4
A
B
C

## Slide 46: Topics – Fault Isolation
How far have you gone with fault isolation?
  Photon Emission Microscopy (PEM)
    Dynamic & Static
  Laser-based Fault Isolation (OBIRCH, LVx)
  Magnetic Field Imaging (MFI)
  Electron Beam Absorbed Current (EBAC)
SEM
EBAC
Source: “Benefits of using a CF4-Free Microwave Induced Plasma (MIP) Spot Etch Process to Remove Underfill and Analyze 2.5D Modules” ISTFA 2020 Proceedings
Source: “Isolating an Open in 2.5D µBump & Chip Bump Chains using SDR, EBAC and Capacitive Measurements” ISTFA 2019 Proceedings

## Slide 47: Topics – Best Destructive Techniques
Use cases for different destructive techniques
  Micro-CNC
  Dry Etches
  Laser Ablation
Sample cleanup needed after certain steps?
Micro-CNC | Dry Etches | Laser Ablation
Remove chips in a 3D/2.5D stack | Remove overmold over interposers, chiplets | 
Polish exposed chips for NIR-based analysis | Expose bumps in cross-section | 

## Slide 48: Topics – Other Techniques
Other techniques that could use more focus
  FIB Editing
    Probe pads
    Cutting lines
    Cross-sectional analysis
  XRAY Tomography
    Resolving smaller features in large form factors
  Through or C-SAM
  TDR and EOTPR
    Is TDR enough to isolate IO defect to specific locations?
    How well can EOTPR isolate a defect and what preparations are needed to achieve that?
  Stress Analysis

## Slide 49
THANK YOU!
Remember…
Take the survey so we can improve.
Join the ASM Connect discussion.
Stay innovative!