## Slide 1
A Comparison of Grain Size Measurement Methods
George F. Vander Voort
Consultant – Struers Inc.

## Slide 2
5/16 Sieve
4 Sieve
8 Sieve
14 Sieve
Separation of grains by sieving after liquid metal embrittlement of  Brass in Hg
Actual Grain Shapes
3.3 mm
3.3 mm
3.3 mm
3.3 mm

## Slide 3
Actual Grain Shapes
SEM secondary electron images of individual  Brass grains separated by liquid metal embrittlement with Hg.
1.1 mm
1.1 mm

## Slide 4
Grain Size Measurement
Types of Grain Sizes
• Non-twinned (ferrite, BCC metals, Al)
• Twinned FCC Metals (austenite)
• Prior-Austenite
(Parent Phase in Q&T Steels)

## Slide 5
ASTM Standards for Grain Size
ASTM E 112: For equiaxed, single-phase grain structures
ASTM E 930: For grain structures with an occasional very large grain
ASTM E 1181: For characterizing duplex grain structures
ASTM E 1382: For image analysis measurements of grain size, any type

## Slide 6
Grain Size Measurements
• Number of Grains/inch2 at 100X: G
• Number of Grains/mm2 at 1X: NA
• Average Grain Area, µm2 : A
• Average Grain Diameter, µm: d
• Mean Lineal Intercept Length, µm: l
_
_
_

## Slide 7
Grain Size Measurement Methods
Comparison Chart Ratings
Shepherd Fracture Grain Size Ratings
Jeffries Planimetric Grain Size
Heyn/Hilliard/Abrams Intercept Grain Size
Triple-Point Count Method
Snyder-Graff Intercept Grain Size
2D to 3D Grain Size Distribution Methods

## Slide 8
Definition of ASTM Grain Size
n = 2 G-1
n = number of grains/in2 at 100X
G = ASTM Grain Size Number

## Slide 9
ASTM Grain Size, G
G | n | G | n
1 | 1 | 6 | 32
2 | 2 | 7 | 64
3 | 4 | 8 | 128
4 | 8 | 9 | 256
5 | 16 | 10 | 512

## Slide 10
Jeffries Planimetric Method
ninside = number of grains completely inside the test circle
nintercepted = number of grains intercepting the circle
NA = f[ ninside + 0.5(nintercepted)]
f = Jeffries multiplier
f = magnification2/circle area

## Slide 11
Jeffries Planimetric Method
Average Grain Area = A = ——
G = (-3.322LogA) – 2.955
1
NA
_

## Slide 12
25 m
Ferritic Stainless Steel Test Structures
Low (100X) and high (400X) magnification views of the ferritic microstructure (left and right), etched for 2 minutes at 1 V dc using aqueous 60% nitric acid. These two images were used for the study. The micrographs were printed with varying size. Test circles of varying size were placed over the images.

## Slide 13
Influence of the Number of Measurements Per Grid Placement on the ASTM Grain Size
It has long been believed that if the counts of grains within the Jeffries test circle is low, the grain size measurement will be biased. But, I have never seen a publication where this variable was evaluated. Is this true?

## Slide 14
Sea Cure 100X 8.71”x 6.62” 6.5” diam. circle

## Slide 15
Sea Cure 100X 8.71”x 6.62” 3.5” diam. circles

## Slide 16
Sea Cure 100X 8.71”x 6.62” 2” diam. circles

## Slide 17
Results for 40 measurements using the E 112 planimetric method with (ninside + 0.5nintercepted) varying from 5 to 444. The linear trend line is almost flat.

## Slide 18
Plot of (ninside + 0.5nintercepted) for values greater than 30. Note that the linear trend line is virtually flat over this range.

## Slide 19
Effect of Test Circles of Low D on G
G is erratic, but not biased to higher or lower values when the count is <10. The linear fit line has a slight upward slope. G values for counts > ~16 yielded results very close to the reference value of G = 6.666

## Slide 20
Saltykov Planimetric Method Using Rectangles
To minimize bias in planimetric grain size measurements when the grains are very large and the number of grains inside the circle gets low, Sarkis A. Saltykov proposed using a rectangle for the grain counts. The grains at the 4 corners are ignore, but are assumed to contribute a total of 1 grain to the count.
The number of grains completely inside the rectangle, ninside, are counted and are weighted as one each. The number of grains that intersect the edges, nintercepted, are counted, but not those at the corners, and are weighted as one-half. Then, NA is determined as:
NA = f[ninside + 0.5nintercepted + 1]
where f is defined as before, M2/A

## Slide 21
Image 5.17 x 6.71”; Rectangle 4 x 4.5”
Planimetric Method Using Saltykov’s Rectangle

## Slide 22
Image 5.17 x 6.71”; Rectangle 2.35 x 3”

## Slide 23
Image 5.17 x 6.71”; Rectangle 1.35 x 1.85”

## Slide 24
Planimetric grain size measurements using rectangles and Saltykov’s counting method for 43 rectangles with (ninside + 0.5nintersected) + 1 values ranging from 2.5 to 790.5. Note that the linear trend line is nearly flat.
Saltykov Planimetric Method Using Rectangles

## Slide 25
Saltykov Planimetric Method With Rectangles, Counts 10
Planimetric grain size measurements using rectangles and Saltykov’s counting method for 23 rectangles with (ninside + nintersected) + 1 values above 10. Note that the linear trend line is flat over this range.

## Slide 26
Effect of Rectangles of Varying Size on G
The Saltykov counting method yields consistent data down to ~11 counts. Note that the linear fit line is horizontal. Note that the G values for counts above ~10 agree very well with the reference values. These results were the best obtained at low counts.

## Slide 27
Saltykov Rectangles, (n1+0.5n2+1) 10
Good estimates of G can be made with (n1+0.5n2+1) as low as 11. The lower limit with test circles using the Jeffries method was 20 - 30.

## Slide 28
Heyn/Hilliard/Abrams Intercept Method
N = number of grains intercepted
P = number of grain boundary intersections
NL = ——
N
LT
PL = ——
P
LT
and LT is the true test line length

## Slide 29
Heyn/Hilliard/Abrams Intercept Method
Mean Lineal Intercept, l = — = ——
1
NL
1
PL
G = [6.644Log10(NL or PL)] – 3.288
G = [-6.644Log10(l)] – 3.288
Note: Units are in mm-1 (for NL and PL) or mm (for l)

## Slide 30
Results for 40 measurements using the E 112 intercept method (but with a single test circle) with Pintersections varying from 6 to 89. The linear trend line is almost flat.
Effect of Varying the P Counts on G

## Slide 31
Plot of Pintersections for values above 20. Note that the linear trend line has a slight downward slope now.
G by the Intercept Method is Better When P>20

## Slide 32
NA = 0.5P + 1
AT
Triple-Point Count Method
where P are triple points within the test circle (4-ray junctions are weighted as 1, rather than as one-half)

## Slide 33
Effect of Varying P per Image on G
Plot of all 41 measurements of P, with a range of 5 to 860, gave a linear fit with a slight downward trend as P increased.

## Slide 34
Flat linear trend for triple point counts above 25 per field (range 35 to 860).
Triple-Points Per Field >25 Gave Constant G

## Slide 35
Jeffries Circle vs Saltykov Rectangle
Although the linear trend line for the Jeffries planimetric method shows a slight downward trend with increasing counts, over the mutual measurement range for the two methods, the data agreement is excellent.

## Slide 36
Comparison of Test Methods
Plot of all data from the planimetric measurements using the Saltykov rectangle and the Jeffries circle compared to the triple-point count method yields a slight downward slope in G with increasing counts.

## Slide 37
Comparison of Methods for Higher Counts
Plot similar to the previous one, but with low count data removed, yielding a flat linear correlation over the data range and excellent agreement between the methods.

## Slide 38
Triple-Point vs Intercept G – Same Count Range
Comparison of the intercept data with the triple-point count data (over only the same range as obtained with the intercept data (6 to 89 P counts). The data agreement is exceptional in that the linear data fit curves are on top of each other over the full range and the trend is flat. The data scatter is greater for counts <30.

## Slide 39
Triple-Point vs Intercept – Low Counts Removed
G Test results are virtually identical when only counts >20 are plotted

## Slide 40
E112 Planimetric | Circles | (n1 + 0.5n2) | No. | Avg. G  95% CL | Std. Dev.
 |  | All (5 to 444) | 40 | 6.823 ± 0.093 | 0.28981
 |  | >120 | 9 | 6.695  0.059 | 0.07689
 |  | >30 | 23 | 6.72  0.0378 | 0.08747
 |  | <30 | 17 | 6.964  0.204 | 0.39729
 |  | <10 | 11 | 6.886  0.313 | 0.46615
Saltykov Planimetric | Rectangles | (n1 + 0.5n2 + 1) | No. | Avg. G  95% CL | Std. Dev.
 |  | All (2.5 to 790.5) | 43 | 6.770 ± 0.088 | 0.28568
 |  | >100 | 8 | 6.703  0.063 | 0.07555
 |  | >50 | 17 | 6.719  0.0519 | 0.10091
 |  | 29 | 20 | 6.722  0.049 | 0.10382
 |  | >10 | 24 | 6.732  0.047 | 0.11129
 |  | <10 | 19 | 6.817  0.199 | 0.41267
E112 Intercept | Circles | Pi | No. | Avg. G  95% CL | Std. Dev.
 |  | All (6 to 89) | 40 | 6.867 ± 0.109 | 0.34165
 |  | 42 | 9 | 6.76  0.11 | 0.14264
 |  | >20 | 23 | 6.76  0.10 | 0.23256
 |  | <20 | 17 | 7.016  0.210 | 0.41083
 |  | <10 | 8 | 6.851  0.437 | 0.52314
Triple Point Count | Circles | Pi | No. | Avg. G  95% CL | Std. Dev.
 |  | All (5 to 860) | 41 | 6.818 ± 0.094 | 0.29638
 |  | >100 | 10 | 6.687 ± 0.039 | 0.05559
 |  | >50 | 24 | 6.699 ± 0.047 | 0.11233
 |  | >25 | 26 | 6.719 ± 0.052 | 0.12848
 |  | <25 | 15 | 6.989 ± 0.228 | 0.41433

## Slide 41
Conclusions
Low counts did not produced an obvious bias in the grain size, G. It did produce data scatter.
 The best grain size measurements were made with the Saltykov rectangle planimetric method yielding constant G with as little is 10 counts per field.
 The Triple-Point count method (rarely used and in no grain size test method), gave excellent G values when the count was >25 per field.
The Jeffries planimetric method gave excellent results when the count was >30 per field.
The intercept method showed a slight variation in G with the count per field and results were best when the count was >40 per field. Experiments at higher counts/field should be done. The intercept method gave slightly poorer results than the other methods.
The agreement in G for the 4 methods was superb (fortunately for us!)

## Slide 42
Measurement of Grain Size for Grains Containing Annealing Twins and When Two Phases or Constituents Are Present

## Slide 43
Intercept Grain Size Example:
Single Phase Twinned Grain Structure
The 100X micrograph is that of a twinned FCC Ni-base superalloy, X-750, in the solution annealed and aged condition after etching with Beraha’s reagent which colored the grains. This is a much more difficult microstructure for intercept counting. The three circles measure 500 mm and P is 63 (intersections with twin boundaries are ignored).

## Slide 44
Intercept Grain Size Example:
Single Phase Twinned Grain Structure
PL = ——— = 12.6 mm-1
63
500/100
l = —— = 0.0794 mm
1
12.6
G = [-6.644Log10(0.0794)] – 3.288 = 4

## Slide 45
Intercept Method for Two-Constituents
N = Number of  grains intercepted
LT = Test line length/Magnification
VV = Volume fraction of the  phase
l = ———
VV(LT)
N

## Slide 46
Intercept Method for Two-Constituents
This 500X micrograph of Ti-6242 was alpha/beta forged and alpha/beta annealed, then etched with Kroll’s reagent. The circumference of the three circles is 500 mm. Point counting revealed an alpha phase volume fraction of 0.485 (48.5%). 76 alpha grains were intercepted by the three circles.

## Slide 47
Intercept Method for Two-Constituents
l = ———————— = 0.006382 mm
(0.485)(500/500)
76
G = [-6.644Log10(0.006382)] – 3.288 = 11.3

## Slide 48
Normal Grain Size Distribution Example

## Slide 49
Motor Lamination Steel
Klemm’s I 100X

## Slide 50
Motor Lamination Steel
Grain Boundary Detection

## Slide 51
Avg. G = 6.63
8 Grain Size Classes
Skew = 1.43 Kurtosis = 2.55 N = 891

## Slide 52
No. Grains |  Grain Areas, m2 | Avg. Grain Area, m2 | ASTM G | No. of G Classes
891 | 1,158,903 | 1300.68 | 6.63 | 8
G | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11
% A | 0 | 3.19 | 23.76 | 42.53 | 20.25 | 7.21 | 2.19 | 0.76 | 0.12
Motor Lamination Steel
Percentage of Grains by Area Per G

## Slide 53
Sea Cure Ferritic Stainless Steel
60% HNO3 at 1.5 V dc, 60 s
Boundary Detection
Grain Interior Detection

## Slide 54
Monit Ferritic Stainless Steel
60% HNO3 at 1.5 V dc, 60 s
Boundary Detection
Grain Interior Detection

## Slide 55
G = 7.14
12 Grain Size Classes
Skew = 1.57 Kurtosis = 2.95 N = 875
The kurtosis number is very close to 3, that of a perfect Gaussian distribution. But, as it covers 12 grain size classes, E 1181, paragraph 8.3.1.2 states that this is a “Wide-Range” random duplex distribution.

## Slide 56
G = 7.48
12 Grain Size Classes
Skew = 2.37 Kurtosis = 8.24 N = 1158
This structure also covers 12 G classes, but the kurtosis is above 5 and according to E 1181, paragraph 8.3.1.2, it is a “Wide-Range” random duplex distribution.

## Slide 57
ASTM G | Secure FSS | Monit FSS
2 | 0 | 0
3 | 0 | 0
4 | 0.8 | 1.44
5 | 20.19 | 12.49
6 | 38.17 | 29.18
7 | 25.62 | 32.62
8 | 11.11 | 17.48
9 | 2.77 | 5.09
10 | 0.88 | 1.24
11 | 0.26 | 0.25
12 | 0.066 | 0.06
13 | 0.042 | 0.053
14 | 0.038 | 0.049
15 | 0.032 | 0.046
Secure and Monit Ferritic Stainless Steels
Percentage of Grains by Area Per G Class

## Slide 58
Grade | No. of Grains |  Of Grain Areas, m2 | Avg. Grain Area, m2 | ASTM G | No. of G Classes | Skew | Kurtosis
Secure | 875 | 798702 | 912.8 | 7.14 | 12 | 1.57 | 2.95
Monit | 1158 | 836879 | 722.7 | 7.48 | 12 | 2.37 | 8.24
Secure and Monit Ferritic Stainless Steels

## Slide 59
Bi-Modal Grain Size Distribution Examples

## Slide 60
Wide-Range Duplex - RA 330 Austenitic Stainless Steel (SA at 1975 F)
100X Detected Grains

## Slide 61
Wide-Range Duplex - RA 330 Austenitic Stainless Steel (SA at 1975 F)
9 Grain Size Classes
Skew = 7.58 Kurtosis = 86.66 N = 416
This structure covers 9 G classes, but the kurtosis is well above 5 and according to E 1181, paragraph 8.3.1.2, it is a “Wide-Range” random duplex distribution.
Avg. G = 6.11

## Slide 62
Wide-Range Duplex - RA 330 Austenitic Stainless Steel (SA at 1975 F)
G | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11
%A | 0 | 5.54 | 8.76 | 12.44 | 30.79 | 21.12 | 12.64 | 5.31 | 1.96 | 0.44 | 0
No. Grains | of Grain Areas, m2 | Avg. Grain Area, m2 | ASTM G (all grains) | No. of G Classes
416 | 776,603.5 | 1866.8 | 6.11 | 9

## Slide 63
Wide-Range Banded Distribution in E-Brite (26-1 Ferritic Stainless Steel)
100X Detected Grains

## Slide 64
47.1%, G = 3.7
52.9%, G = 6.5
No. of G Classes = 14
Skew = 3.59 Kurtosis = 18.62 N = 339
The kurtosis is high, but the difference in the G values is <3 GS numbers. I would tend to call it a “Wide-Range” random duplex condition.

## Slide 65
G | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15
%A | 0 | 3.5 | 16.3 | 24.4 | 20.6 | 17.4 | 10.4 | 3.7 | 0.7 | 0.1 | 0.08 | 0.008 | 0.011 | 0.004 | 0.003
E-Bright (26-1) Ferritic Stainless Steel – Wide-Range Bi-Modal Distribution
No. Grains | of Grain Areas, m2 | Avg. Grain Area, m2 | ASTM G (all grains) | No. of G Classes
339 | 804976.1 | 2374.6 | 5.7 | 14

## Slide 66
SCF-19 Austenitic Stainless Steel - Necklace Type Bi-Modal Distribution
100X Detected Grains

## Slide 67
71.54%, G = 4.4
28.46%, G = 11.5
14 Grain Size Classes
Skew = 14.84 Kurtosis = 254.5 N = 3895

## Slide 68
G | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15
% A | 0 | 12.4 | 24 | 15.6 | 10.3 | 7.62 | 2.93 | 2.29 | 4.53 | 6.34 | 6.24 | 4.25 | 2.11 | 0.98 | 0.39
SCF-19 Austenitic Stainless Steel – “necklace” Type Bi-Modal Distribution
No. of Grains |  Of Grain Areas, m2 | Avg. Grain Area, m2 | ASTM G (All Grains) | No. of G Classes
3895 | 579832.8 | 148.87 | 9.76 | 14

## Slide 69
Experimental Alloy 625 – “Necklace” Type Topological Duplex Grain Size Distribution
100X Grain Detection

## Slide 70
70.47% at G = 2.95
29.53% at G = 9.29
15 Grain Size Classes
Skew = 9.65 Kurtosis = 96.93 N = 1073
The kurtosis is very high. This is clearly a “necklace” type “Topological” duplex distribution. The difference between the two avg. G values is 6.33, much more than 3 (per 8.3.2.2). It is clearly bi-moddal, but is not classified as bi-modal.

## Slide 71
Experimental Alloy 625 – Bi-Modal “Necklace” Distribution
G | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15
% A | 0 | 7 | 26.2 | 22.9 | 10.8 | 3.53 | 8.59 | 9 | 6.19 | 2.92 | 1.38 | 0.65 | 0.27 | 0.2 | 0.18 | 0.13
No. Grains |  Of Grain Areas, m2 | Avg. Grain Area, m2 | ASTM G (All Grains) | No. G Classes
1073 | 726007.7 | 676.6 | 7.58 | 15

## Slide 72
Low-Carbon Steel with ALA Bi-Modal Grain Size Condition
100 X Finer Grains Detected

## Slide 73
One at G = 2.4 and one at G = 3.1
G = 11.1
Skew = 70.7 Kurtosis = 5717.9 N = 11624

## Slide 74
G | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15
% A | 0 | 3.4 | 2 | 0 | 1.14 | 0.7 | 0.86 | 2.86 | 20.0 | 34.0 | 23.2 | 7.08 | 1.54 | 1.9 | 1.15
Low-Carbon Steel “ALA” Bi-Modal Distribution
No. Grains |  of Grain Areas, m2 | Avg. Grain Area, m2 | ASTM G (All Grains) | No. of G Classes
11624 | 735616.14 | 63.27 | 10.99 | 14

## Slide 75
Conclusions
There are several ways to measure the grain size of single-phase microstructures and they give the same results within statistical precision.
Measuring grain size in twinned grains is difficult as the twin intersections must be ignored.
Two-phase/constituent microstructures can be evaluated but the area fraction is needed.
Grain size distribution analysis can tell us if the distribution is Gaussian or bi-modal.